## Slide 1: Evaluation of SOG film by Dilution ratio
Hoseo Univ.
Electronic Device Lab.
Undergraduate 3th student.
SANG MIN LEE
李 相 旼
Notes: Hello everyone!
My name is SANGMIN LEE at a undergraduates 3rd grades at Digital display engineering, hoseo university
I am very glad to be here.

## Slide 2: Content
1. Introduction
2. Experiment
3. Result
4. Conclusion
Notes: The table of contents consists of introduction, experiment, result and conclusion.

## Slide 3: Introduction
The solution process can reduce the process time and cost.
The SOG is the solution process to get Silicon Oxide.
A SOG film was formed with MOS structure according to the dilution ratio of SOG to IPA.
Notes: First, let me introduce the experiment.
The solution process can reduce the process time and cost.
The SOG is the solution process to get Silicon Oxide.
A SOG film was formed with MOS structure according to the dilution ratio of SOG to IPA.

## Slide 4: Experiment
The diluted SOG solution was spin-coated for an insulator film.
The MOS structure was fabricated and C-V , Breakdown voltage, Leakage current were measured.
Dilution ratio | Material | Coating counts | Thickness
100% | SOG 40ml | 1 | 340nm
50% | SOG 20mL + IPA 20ml | 2 | 330nm
25% | SOG 10ml + IPA 30ml | 5 | 315nm
Table 1. SOG dilution with IPA
Notes: It’s my purpose to the evaluation of SOG film by dilution ratio.
So, I Spin-coated diluted SOG solution for an insulator.
And, The MOS structure was fabricated and C-V, Breakdown voltage, Leakage current were measured.
The Solutions was prepared by diluting with IPA.

## Slide 5: Experiment
Spin Coater
3,000 rpm, 30 s.
1. Cleaning
P-type Si wafer
2. SOG Coating
4. Annealing
Furnace
450 ℃ / 1 h. / N2
180 ℃ 20 m.
80 ℃ 5 m /
5. Metal Deposition
P-type Si wafer
Sputter
Pre Sputtering 100 s.
Sputtering 400 s.
6. Evaluation
P-type Si wafer
Metal(Al), wafer
Contact and Evaluation
3. Bake
Figure 1. MOS structured devide fabrication process
Hot plate
130 ℃ 5 m /
Experiment
Notes: And then, this slide shows the experiment before more detail proceeded in this order.First, p-type silicon wafer was cleaned with a Nitrogen gun.
Next, the device that is coated with SOG insulator using spin coater.
Coating at 3000 rpm for 30 seconds will coat the insulator with a thickness of 3400 angstroms.
The coated device is then baked at 80 degree C for 5 minutes and 130 degree C for 5 minutes and 180 degree C for 20 minutes.Next, it is furnace annealed at a temperature of 450 degree C for 1 hour in nitrogen ambient.
After the annealing process, covered a shadow mask on the device and deposit to Aluminum Silicon on top of the insulator using a sputter.The size of the electrode was a circular shape with a radius of 0.8mm.And next, pre sputtering time 200 seconds, and sputtering time 400 seconds.
And next, the C-V, L/C, VB are measured by contacting AlSi deposited on top of the fabricated device and p-type silicon wafer having a common electrode formed on the bottom.

## Slide 6: Result
Figure 2. The C-V curves are shown according to the dilution ratio.
Dielectric constant | Dilution ratio | Electrode radius 0.8mm
Dielectric constant | 100% | 1.18
 | 50% | 1.68
 | 25% | 2.99
Notes: To the next, this slide shows result of the Capacitance for the diluted solution, respectively.In the table below, the K value is calculated as follows.
As the IPA dilution concentration increased, the curve area was identified and the value of the dielectric constant was also increased.

## Slide 7: Result
Figure 3. The leakage current densities according to the dilution ratio.
Notes: And this slide shows this slide shows result of the leakage current for the diluted solution, respectively.
In case of SOG 100%, the leakage current of device is high.
When SOG 50% + IPA 50% and SOG 25% + IPA 75% are compared, it can be seen that the leakage current of SOG 25% + IPA 75% is slightly small.

## Slide 8: Result
Figure 4. The breakdown voltages were measured according to the dilution ratio.
Notes: And next, this slide shows result of the VB for the diluted solution, respectively.
In general, it can be seen that the SOG 100 % insulator does not break even when applied to about 3 [MV / cm], it was confirmed that a high current flow.
In case of SOG 50% + IPA 50%, breakdown occurred under 2 [MV/cm], but in most cases, breakdown occurred in more than 2 cases in SOG 25% + IPA 75%.

## Slide 9: Conclusion
SOG was diluted with IPA and coated. The dilution effect was studied.
Since the diluted film becomes thinner, it is deposited several times to adjust the thickness of the film to a certain thickness.
The leakage current of the SOG film deposited by dilution was less than undiluted SOG film.
It is preferable to use diluted SOG solution for an insulating film of a thin film transistor.
Notes: SOG was diluted with IPA and coated. The dilution effect was studied.
Since the diluted film becomes thinner, it is deposited several times to adjust the thickness of the film to a certain thickness.
The leakage current of the SOG film deposited by dilution was less than undiluted SOG film.
It is preferable to use diluted SOG solution for an insulating film of a thin film transistor.

## Slide 10: Thank you for your attention!
Notes: Hello everyone!
My name is SANGMIN LEE at a undergraduates 3rd grades at Digital display engineering, hoseo university
I am very glad to be here.