## Slide 1: Insulator Characteristics of Solution Al2O3
18.01.13
Junior in HOSEO University
Electronic Display Engineering
Hong, Seung Hyun
洪承鉉

## Slide 2: Contents
Introduction
-Solution process
-Solution meterial
Experiment
Result
Conclusion
Future research

## Slide 3: Solution process
Advantage
  Inexpensive costs
  Saving time
  Low temperature
Disadvantage
  Not good membranous
  Less stability

## Slide 4: Solution Selection(Al2O3)
A high Dielectric constant
Large band gap (8.7 ev)
Excellent electrical insulation (1x1015 Ωcm)
High heat resistance

## Slide 5: Experiment
0.2M solution
  - Al(NO3)3.9H2O 0.755g / DMAC 20mL
  - Equipment - stirrer
    Temperature - 100℃
    Velocity - 1000rpm
    Time - 72hour

## Slide 6: Experiment
wafer
O2 Plasma
O2
O2
O2
O2
O2
wafer
Al2O3
wafer
Al2O3
solvent
O2/Plasma treatment
1min
Spin coater
500rpm 30sec
1000rpm 30sec
1500rpm 30sec
Soft baking
60°C 5min > 70°C 5min > 80°C 5min > 90°C 5min
wafer
Al2O3
wafer
Al2O3
Al
Al
Hard baking
300° 1hour
Sputtering
Pre sputter 300sec
Sputter 600sec

## Slide 7: Result
 | 500rpm | 1000rpm | 1500rpm
Coating state |  |  | 

## Slide 8: Result
 | 100°C | 200°C | 300°C | 400°C
I-V Leakage |  |  |  | 
I-V Breakdown voltage |  |  |  | 

## Slide 9: Conclusion
In this experiment, insulation film was made using an aluminum oxide solution and the characteristics were compared according to RPM and hard baking temperature.
The leakage current was improved according to the hard baking temperature and the breakdown voltage was increased from around 100V to 140V.
400 degree hard baking and 1500 RPM coating conditions gave the best performance and we saw the potential for them to be applied to a gate insulator.

## Slide 10
Thank you